## Slide 1
BACKGROUND
  Manganite based bipolar RRAM is an attractive prospect for non-stochastic switching, area-dependent current scaling, fast switching and long endurance, forming-less operation. [1,2]
  Different mechanisms of switching have been proposed like interface resistance switching [3], SCLC [4] and Metal – Insulator Mott-Transition [5]. Exponential Distribution of traps have been proposed in similar devices(Ag/La0.7Ca0.3MnO3/Pt)[6].
OBJECTIVE
We confirm SCLC as the transport mechanism
We extract materials parameters like spatial and energy distribution of traps by deriving simple analytical expressions from experimental I-V characteristics.
FABRICATION AND I-V CHARACTERIZATION
Process Flow
I-V Characterization
HRS resistance and Set Voltage(Vset) increase with increase in Vreset.
CURRENT TRANSPORT REGIMES AND MODELS
CURRENT REGIMES
PARAMETER EXTRACTION
Materials Parameter Extraction using Analytical Models in PCMO based RRAM
I. Chakraborty, A. K. Singh, P. Kumbhare, N. Panwar, U. Ganguly
CEN, Department of Electrical Engineering, IIT Bombay, Mumbai 400076, India
CONCLUSIONS
Developed analytical models based extraction of materials parameters for PCMO RRAM
Energy and spatial distribution of trap-density is extracted.
Results estimate an almost uniform (NT~1017/cc) single trap-level(ET –EV~0.15eV)
Model provides consistent trap-density estimated from low-bias Ohmic regime as well as high-bias trap-filled limit.
REFERENCES
S. Park et al, Phys. Status Solidi RRL 5
N. Panwar et al, MRS (Fall), 2013.
S. Jung et al, IEDM 2011
T. Harada et al, APPLIED PHYSICS LETTERS 92, 222113 (2008)
H. S. Lee et al, Nature Scientific Report, 2013.
D. S. Shang et al, PHYSICAL REVIEW B 73, 245427 (2006)
M. Lampert., Reports on Progress in Physics 27.1 (1964): 329.
N. Biškup et al, PHYSICAL REVIEW B 72, 024115 (2005)
S. Zhigao et al., Nature communications 3 (2012): 94
. Herpers et al, Adv. Mater. 2014.
J. G. Simmons, PHYSICAL REVIEW LETTERS, Volume 23, Number 6, 1969.
Regimes | Slope(α) | Equation[7]
1. Ohmic | ~1 | 
2. Trap SCLC | ~2 | 
3. Trap-filled Limit | >>2 | 
4. Trap-free SCLC | ~2 | 
Asymmetry in current levels observed between –ve and +ve polarity for both HRS and LRS.
Various trap concentration profiles simulated
Trap profile of gentle asymmetry of 2-4× can produce the polarity dependent current asymmetry of 1.2×, of the same order as experimental
Fairly uniform trap distribution assumption validated.
MOTIVATION
+ :
I-V ASYMMETRY & NON-UNIFORM NT
J ~Vα
Assumptions: 1. Single energy trap level with uniform spatial distribution 2. Permittivity(ε) ~ 30-40 [8,9]
Step 1: Mobility estimate: gives us thus
Step 2: NT estimate (method 1):
  NT estimate (method 2):
Using Poisson,
Charge concentration:
RESULTS
Trap Depth(ET-EV) | Remains Constant(LRS) Negligibly rises(HRS) | With increasing Vreset
NT-Ohmic and NT-TFL increases linearly with increasing Vreset
Linear correlation between NT-Ohmic and NT-TFL (R2=0.9921)
Single trap level assumption validated
Trap densities at low and high bias are consistent
METHODOLOGY
DERIVATION OF NT-OHMIC [11]
φmax is assumed to be at the center of the device
BAND PROFILE
Si/SiO2 substrate
Pt(57nm)/Ti(9nm) deposited on substrate
50nm layer of Pr0.7Ca0.3MnO (PCMO) deposited at room temperature(using PLD)
Annealed in N2 at 6500C for 120 s
Tungsten probe-tips formed the top electrode
Constants
[10]
Constants
ACKNOWLEDGEMENTS
Funded by -
Department of Science and
Technology (DST),
Government of India